# Installation on a concrete or asphalt base

- Preparation of the substructure:

### The substructure has to be clean, dry and free of dust

- Existing concrete or asphalt flooring tile:

sweep all the surface or clean it with high pressure jet of water if necessary. In this case: wait until all the water has evaporated before starting to glue.

- New concrete flooring tile:

respect the complete drying delay and the 21 days of milt before beginning to glue.

- New asphalt flooring tile:

remove all oils of the asphalt before starting to glue.

- Preparation of the glue and gluing of the substructure:

The glue furnished by rbsi is a bi – component polyurethane glue with single gluing.

It’s packed in a kit including:

- kit of 6 kg: 1 pot of base of 5.4 kg (A) + 1 pot of hardener of 0.6 kg (B)

- kit of 12.2 kg: 1 pot of base of 11 kg (A) + 2 pot of hardener of 0.6 kg (B)

Prepare one kit at once according to the progression. Do not prepare all the glue in a big drum in one time: the mixture can only be used during 20 to 45 minutes at a temperature of 20°C.

a. Pour all of part B in part A, mix with a mixer at slow speed (max 400 tr/min) until obtaining an unctuous and homogeneous mixture.

b. Apply the glue uniformly with a notched scraper (by dry weather, moderate temperature and only on a dry ground). Do not glue by piles.

Recommended proportioning: +/- 1 kg/m² on asphalt.

Apply by dry weather – temperature between 15°C and 35°C

- Further information

  - Verify the efficiency of the rain water evacuation and the flowing system, especially if the application of the glue obstructs a porous ground.

  - Take in account the polymerisation time of the glue, time during which the ground doesn’t have to undergo climatic and mechanical aggression.

Solidification: between 4 and 6 hours

## Opening to walk: 6 hours

Definitive polymerisation: 4 days

- Take in account the dimensional variation of the covers under the action of climatic changes: it would be better to glue all the surface in one time and avoid the periods with big range of temperature (f.e. hot day, cold night)

- It’s strongly advised against gluing the tiles if it risks to rain during the 6 hours following the installation.

We stay at your disposal for all information you may require.